- The Hunter Eco-Wrap shall be pre-assembled and constructed with a wrapping of special polypropylene fleece material and pressure-compensating, non-draining inline emitter tubing.   The wrapped emitter tubing shall have a nominal outside diameter of 16mm and shall have 0.6 GPH (2,3 l/h) emitters. Emitters shall be uniformly spaced at 12 in (30 cm) intervals. Tubing shall be constructed to landscape grade specifications with a nominal wall thickness not less than 1.1mm and a UV protection rating of seven years.   Each roll of Eco-Wrap shall be 100 m in length. The rolls shall be delivered with solid caps inserted to protect the tubing from debris during installation.

- The Eco-Wrap subsurface irrigation system shall be manufactured for Hunter Industries Incorporated, San Marcos, California.